## Slide 1: Things thought about and decided on choosing certain plots, etc.

## Slide 2
In considering a more comprehensive (including 619 etc.) version of this plot, I looked at the 2014-09-16 data, but nothing is quite as good. The 40K deposit for run 77 etc. is not similar to the other ones, because this day had long WL deposits. Here is a comparison of same-excitation for 11 K and 40 K, but again I don’t think they’re similar enough, and you should just use a separate day’s tests for seeing the 619 magnitude vs. deposit temp.

## Slide 3
On deciding what to call the leak rate for leak44 (for 619 leak rate dependence):
2014-07-29, the data used for leak rates in BaSpec, give:
Leak50 120 nm/s
Leak48 55 nm/s
Leak46 30 nm/s
Leak44 8 nm/s but these are not exactly right due to neglect of SXe n
Those are at 11 K. For quoting at ~50 K, multiply by (31/37) based on recent test. Then, to get the real leak rate, multiply above numbers by (37/55) since leak 48 was measured to be 37 nm/s at 11 K in recent stuff (rather than 55 nm/s).
But since the thing in the thesis is describing the leak rate 44 at 11 K, just do:
(8 nm/s) х (37/55) ≈ 5 nm/s.

## Slide 4
On 693 peak(s)
This was misleading because the grating
was at different places (and uncalibrated):
~100 K
~15 K
The old paper was at 77 K, so… idk
What really seems to happen is that the lower-wavelength one goes away between ~100 K and ~15 K (T measurements aren’t really good for this, but that’s close):
Cooling from room temp does this