## Slide 1: Things thought about and decided on choosing certain plots, etc. also just production processes

## Slide 2
In considering a more comprehensive (including 619 etc.) version of this plot, I looked at the 2014-09-16 data, but nothing is quite as good. The 40K deposit for run 77 etc. is not similar to the other ones, because this day had long WL deposits. Here is a comparison of same-excitation for 11 K and 40 K, but again I don’t think they’re similar enough, and you should just use a separate day’s tests for seeing the 619 magnitude vs. deposit temp.

## Slide 3
On deciding what to call the leak rate for leak44 (for 619 leak rate dependence):
2014-07-29, the data used for leak rates in BaSpec, give:
Leak50 120 nm/s
Leak48 55 nm/s
Leak46 30 nm/s
Leak44 8 nm/s but these are not exactly right due to neglect of SXe n
Those are at 11 K. For quoting at ~50 K, multiply by (31/37) based on recent test. Then, to get the real leak rate, multiply above numbers by (37/55) since leak 48 was measured to be 37 nm/s at 11 K in recent stuff (rather than 55 nm/s).
But since the thing in the thesis is describing the leak rate 44 at 11 K, just do:
(8 nm/s) х (37/55) ≈ 5 nm/s.

## Slide 4
On 693 peak(s)
This was misleading because the grating
was at different places (and uncalibrated):
~100 K
~15 K
The old paper was at 77 K, so… idk
What really seems to happen is that the lower-wavelength one goes away between ~100 K and ~15 K (T measurements aren’t really good for this, but that’s close):
Cooling from room temp does this

## Slide 5
Achieving the surface BG spectrum:
The reason to multiply the sapphire part by 0.6 is that it should not be larger than the black spectrum (which is surfBG + sapp). The surface part has less sapp in it because it is tapering off there, so it needs scaling, and this is sort of the best guess, albeit not necessarily correct – however, the sapp contribution in the region we care about is small anyway.
unscaled

## Slide 6
I cannot find the code for re-binning plots, so I for-went this one:

## Slide 7
5 × average(abs(x/y pos minus that of previous run))
8-7 x .741 μm
9-16 x .484 μm y .62 μm
ignored 8-7 y due to cam warming
Determining the “typical variance” of laser position in image:

## Slide 8
Determining stat. and syst. errors on these
Stat error = 1.08/sqrt(6) = 0.44
Stat error = 0.827/sqrt(4) = 0.41
Systematic errors come from the horrible equation in fringe_interference.xlsx, and come from just inputting the central values for T:
And for the full error I just did quadrature sum
0.31 and 0.35

## Slide 9
Value/uncertainty on difference between x and y focus w/ no astig. corr.
127.59 ± 2.5 μm
From quadrature adding of the two uncertainties

## Slide 10
Expected and Observed in Scanning
Expected signal from 20150807, / mW,
with #atoms definition #2 (x2 2.06μm×2.06μm region):
1000
or 200 cts/atom
trend line:
Next: consider these (in 1D/ of 8-12 and 8-21), and you had a script that plots them on the same plot, and you could observe things like (a) failure to match up for BG sub – what does that mean? (b) fluctuations are lower than they appeared in the 2D plots, …(c) is it lower in the bleached region of 8-21? …
Goal:
ation
Another question, since maybe the variations aren't as big as you thought, is are those peaks possibly actually atoms, in the ones that had a cool peak

## Slide 11
lin
2015-05-26 is plotted just for the ones before the Xe variations

## Slide 12
On calibration of 2014-06-26 (bleaching) data:
Spectrum from output I sent Brian (pretty sure) for the BaSpec paper
From this (20140916), just scaled up, and this is calibrated (by program, but permanently)
Graph-calibrated by recal_map.txt and function cal20140626() from spec_calibrate.C
It’s off a little bit on the 577 peak for some reason, but that’s just how it is.

## Slide 13
On the bleaching data:
They appear to be v2, which is integrals of the fit peaks, not power-scaled.

## Slide 14
On re-pump using Kr laser:
These saw only the destruction w/ higher Kr
Appears to be an effect!
…but is it actually due to a higher baseline?
This thing does NOT appear in set 1 runs
Especially since the powers are supposedly similar between these “re-pumps” and the most destructive case in the earlier ones, this seems to be not real. One difference between sets 1 and 2 is the dep. temp., but this doesn’t explain the weird baseline thing – maybe there were differences I couldn’t easily pick out of the notes. Weird conditions were being tried to mimic those of the old separate Kr re-pumps.
Not sure what that is, cuz it’s not in the BG apparently… see above summary.

## Slide 15
On re-pump: IR powers
There are zero notes on the IR power on 20131130. 20131216 saw no effect of the IR lasers, even though one run had no filters on it. This makes me suspect that it was not aligned properly, since a negative effect was evident on 20131130 with IR lasers
On re-pump: scaling and shifting of the ones use
The timing of 12-16 were shifted to begin at 96.whatev, like 11-30, which is more correct.
And the overall counts were scaled x3.5 to be more like the green-only run which compares more properly to 11-30 (Kr ones may start out lower due to fast bleaching). After that, it agrees more closely with the 3-s DC vs. 6-s DC.
On re-pump laser intensities
Assuming the same 600 micron w, which is probably OK since it’s defocused 10x more than the focal position differences.

## Slide 16
On power meter QE (2014-08-15):
~70% was obtained in the green, but this is consistent with the power meter’s sensitive area vs. the ~7-mm green w on the optical table. Blue was more like 50%, but I don’t know its size at the optical table. Basically the data is useless because we didn’t write down where the power meter was.

## Slide 17
On cryo-vibration area multiplier:
2.06×2.66μm w is around 40 μm2 over 1/e, which is 4.65× the laser spot size of 8.6 μm2, and I wrote 5× in the thesis... May have changed to 4.7
5×5μm w is around 122 μm2 over 1/e, which is 3.1× the laser spot size of 39.3 μm2.
(bi-convex lens)
2.5× for 6.7×6.7μm